## Slide 1: RTD
Ref. | Frequency (GHz) | Tuning range (%) | Single/ Array | Output power (dBm) | PDC (W) | DC-to-RF efficiency (%) | Phase noise (dBc/Hz) | Chip area (mm2) | On-chip ant. | Beam forming | Technology/ Country | Year | Other properties
1 | 450 | n/a | 36 array | 10.72 | 1.12 | 1 | n/a | 10.24 | 23.9 dB (w/o Si Lens ) | n/a | InP RTD/ Japan | 2022 | 3 dB beam width: 13º
2 | 1090 | n/a | 2 array | -20.46 | n/a | n/a | n/a | n/a | Yes. (w/o Si Lens ) | n/a | InP RTD/ Austria | 2022 | 
3 | 260 | n/a | single | 0 | n/a | 0.7 | n/a | 0.12 | No | n/a | InP RTD/ UK | 2020 | 
4 | 1980 | n/a | single | -43.98 | n/a | n/a | n/a | n/a | Yes. (w/ Si Lens ) | n/a | InP RTD/ Japan | 2017 | 
5 | 1920 | n/a | single | -33.98 | n/a | n/a | n/a | n/a | Yes. (w/ Si Lens ) | n/a | InP RTD/ Japan | 2016 | 
6 | 1000 | n/a | 89 array | -1.37 | 10.92 | 0.007 | n/a | n/a | Yes. (w/o Si Lens ) | n/a | InP RTD/ Japan | 2019 | 
6 | 1040 | n/a | single | -14.32 | 0.03 | 0.11 | n/a | n/a | Yes. (w/o Si Lens ) | n/a | InP RTD/ Japan | 2019 | 
7 | 1420 | n/a | single | -30 | n/a | n/a | n/a | n/a | Yes. (w/ Si Lens ) | n/a | InP RTD/ Japan | 2014 | 
8 | 1790 | n/a | single | -40 | n/a | n/a | n/a | n/a | Yes. (w/ Si Lens ) | n/a | InP RTD/ Japan | 2019 | 
9 | 548 | n/a | single | -3.77 | n/a | 0.01 | n/a | n/a | Yes. (w/ Si Lens ) | n/a | InP RTD/ Japan | 2011 | 

## Slide 2: RTD
Ref. | Frequency (GHz) | Tuning range (%) | Single/ Array | Output power (dBm) | PDC (W) | DC-to-RF efficiency (%) | Phase noise (dBc/Hz) | Chip area (mm2) | On-chip ant. | Beam forming | Technology/ Country | Year | Other properties
10 | 620 | n/a | 2 array | -2.15 | n/a | n/a | n/a | n/a | Yes. (w/ Si Lens ) | n/a | InP RTD/ Japan | 2013 | 
10 | 770 | n/a | 2 array | -5.69 | n/a | n/a | n/a | n/a | Yes. (w/ Si Lens ) | n/a | InP RTD/ Japan | 2013 | 
10 | 810 | n/a | 2 array | -7.45 | n/a | n/a | n/a | n/a | Yes. (w/ Si Lens ) | n/a | InP RTD/ Japan | 2013 | 
11 | 1520 | 2.34 | 3 array | -27.21 | 0.0116 | 0.0164 | n/a | 0.24 | Yes. (w/o Si Lens ) | n/a | InP RTD/ Korea | 2015 | 
12 | 675 | n/a | 2 array | -13.28 | 0.0141 | 0.33 | n/a | 0.11 | 0.3 dBi (w/o Si Lens ) | n/a | InP RTD/ Korea | 2016 | 
13 | 1111 | n/a | single | -40 | n/a | n/a | n/a | n/a | Yes. (w/o Si Lens ) | n/a | InP RTD/ Austria | 2011 | membrane
14 | 1220 | n/a | single | -21.55 | n/a | n/a | n/a | n/a | Yes. (w/ Si Lens ) | n/a | InP RTD/ Japan | 2021 | 
15 | 500 | n/a | single | -6.58 | n/a | n/a | n/a | n/a | Yes. (w/ Si Lens ) | n/a | InP RTD/ Japan | 2022 | 
16 | 1310 | n/a | single | -20 | n/a | n/a | n/a | n/a | Yes. (w/ Si Lens ) | n/a | InP RTD/ Japan | 2012 | 
17 | 350 | n/a | 2 array | -15.09 | n/a | n/a | n/a | n/a | Yes. (w/ Si Lens ) | n/a | InP RTD/ Japan | 2021 | 

## Slide 3: RTD
Ref. | Frequency (GHz) | Tuning range (%) | Single/ Array | Output power (dBm) | PDC (W) | DC-to-RF efficiency (%) | Phase noise (dBc/Hz) | Chip area (mm2) | On-chip ant. | Beam forming | Technology/ Country | Year | Other properties
18 | 692 | n/a | single | --20.32 | 0.0034 | 0.274 | n/a | 0.114 | Yes. (w/o Si Lens ) | n/a | InP RTD/ Korea | 2021 | 
19 | 330 | n/a | 2 array | -11.55 | n/a | n/a | n/a | n/a | Yes. (w/o Si Lens ) | n/a | InP RTD/ Austria | 2021 | 
20 | 84 | 0.18 | 2 array | 3.01 | 0.114 | n/a | n/a | n/a | No | n/a | InP RTD/ UK | 2018 | 
21 | 62.5 | n/a | single | 5 | 0.0233 | n/a | n/a | n/a | No | n/a | InP RTD/ Sweden | 2014 | RTD-MOSFET
22 | 1550 | n/a | single | -33.98 | n/a | n/a | n/a | n/a | Yes. (w/ Si Lens ) | n/a | InP RTD/ Japan | 2014 | 
23 | 1040 | 4 | single | -21.55 | n/a | n/a | n/a | n/a | Yes. (w/ Si Lens ) | n/a | InP RTD/ Japan | 2010 | 
24 | 613 | 1.14 | single | -19.21 | n/a | n/a | -95 | n/a | Yes. (w/ Si Lens ) | n/a | InP RTD/ Japan | 2018 | Varactor. Phase Noise, OffSet: 100KHz
25 | 640 | 20 | single | n/a | n/a | n/a | n/a | n/a | Yes. (w/ Si Lens ) | n/a | InP RTD/ Japan | 2016 | Varactor 4 Array Tuning Range: 580~900 GHz
26 | 655 | 11 | single | -21.74 | n/a | n/a | n/a | n/a | Yes. (w/ Si Lens ) | n/a | InP RTD/ Japan | 2014 | Varactor
27 | 985 | 10 | single | -30 | n/a | n/a | n/a | n/a | Yes. (w/ Si Lens ) | n/a | InP RTD/ China | 2021 | 

## Slide 4: RTD
Reference
Y. Koyama et al., "A High-Power Terahertz Source Over 10 mW at 0.45 THz Using an Active Antenna Array With Integrated Patch Antennas and Resonant-Tunneling Diodes," IEEE Trans. Terahertz Sci. Technol., 2022.
P. Ourednik et al., "Double-resonant-tunneling-diode bridge-less patch-antenna oscillators operating up to 1.09 THz," Appl. Phys. Lett., vol.120, no.18, 2022.
A. Al-Khalidi et al., "Resonant Tunneling Diode Terahertz Sources With up to 1 mW Output Power in the J-Band," IEEE Trans. Terahertz Sci. Technol., vol. 10, no. 2, pp. 150-157, 2020.
R. Izumi et al., "1.98 THz resonant-tunneling-diode oscillator with reduced conduction loss by thick antenna electrode," 42nd Int. Conf. Infrared Millimeter Terahertz Waves, pp. 1–2, 2017.
T. Maekawa et al., "Oscillation up to 1.92 THz in resonant tunneling diode by reduced conduction loss," Appl. Phys. Exp., vol. 9, no. 024101, 2016
K. Kasagi, et al., "Large-scale array of resonant tunneling-diode terahertz oscillators for high output power at 1 THz," J. Appl. Phys., vol. 125, no. 151601, 2009.
H. Kanaya et al. "Fundamental Oscillation up to 1.42 THz in Resonant Tunneling Diodes by Optimized Collector Spacer Thickness," J Infrared Milli Terahz Waves vol. 35, pp. 425–431, 2014.
R. Izumi et al., "Resonant-tunneling-diode terahertz oscillator with a cylindrical cavity for high-frequency oscillation," AIP Advances, vol. 9, no. 8, 085020, 2019.
K. Hinata et al., "High output power (∼ 400μW) oscillators at around 550 GHz using resonant tunneling diodes with graded emitter and thin barriers," Appl. Phys. Exp., vol. 4, no. 6, 064101, 2011.
S. Suzuki, M. Shiraishi, H. Shibayama, and M. Asada, "High-power operation of terahertz oscillators with resonant tunneling diodes using impedance-matched antennas and array configuration," IEEE J. Sel. Topics Quantum Electron., vol. 19, no. 1, pp. 8500108–8500108, 2013.

## Slide 5: RTD
Reference
J. Lee, M. Kim, and K. Yang, "A 1.52 THz RTD triple-push oscillator with a μW -level output power," IEEE Trans. THz Sci. Technol., vol. 6, no. 2, pp. 336–340, 2016.
M. Kim, J. Lee, J. Lee, and K. Yang, "A 675 GHz differential oscillator based on a resonant tunneling diode," IEEE Trans. THz Sci. Technol., vol. 6, no. 3, pp. 510–512, 2016.
M. Feiginov et al., "Resonant-tunnelling- diode oscillators operating at frequencies above 1.1 THz," Appl. Phys. Lett., vol. 99, pp. 233506-1–233506-3, 2011.
X. Yu, et al. , "Highly efficient resonant tunneling diode terahertz oscillator with a split ring resonator," IEEE Electron Device Lett., vol. 42, no. 7, pp. 982–985, 2021.
M. Van Ta et al. "Structure dependence of oscillation characteristics of structure-simplified resonant-tunneling-diode terahertz oscillator," Appl. Phys. Exp., vol.15, no. 4, 042003, 2022.
H. Kanaya et al., "Fundamental oscillation up to 1.31 THz in resonant tunneling diodes with thin well and barriers," Appl. Phys. Exp., vol. 5, no. 12, 124101, 2012.
S. Iwamatsu et al., "Terahertz coherent oscillator integrated with slot-ring antenna using two resonant tunneling diodes," Appl. Phys. Express, vol. 14, pp. 034001-1–034001-4, 2021.
J. Lee, M. Kim, and J. Lee, "692 GHz high-efficiency compact-size InP based fundamental RTD oscillator," IEEE Trans. Terahertz Sci. Technol., vol. 11, no. 6, pp. 716–719, 2021.
P. Ourednik et al., "Double-resonant-tunneling-diode patch-antenna oscillators," Appl. Phys. Lett., vol. 119, pp. 263509-1-263509-5, 2021.
J. Wang et al., "15-Gb/s 50-cm wireless link using a high-power compact III-V 84-GHz transmitter," IEEE Trans. Microw. Theory Techn., vol. 66, no. 11, pp. 4698–4705, 2018.
L. Ohlsson et al., "A 15-Gb/s Wireless ON-OFF Keying Link," IEEE Access, vol. 2, pp. 1307-1313, 2014.

## Slide 6: RTD
Reference
T. Maekawa et al. "Frequency increase in terahertz oscillation of resonant tunnelling diode up to 1.55 THz by reduced slot‐antenna length.", Electron. Lett., vol. 50, no. 17, pp. 1214-1216, 2014.
S. Suzuki et al., "Fundamental oscillation of resonant tunneling diodes above 1 THz at room temperature," Appl. Phys. Lett., vol. 97, no. 24, 242102, 2010.
K. Ogino et.al., "Spectral Narrowing of a Varactor-Integrated Resonant-Tunneling-Diode Terahertz Oscillator by Phase-Locked Loop, " J. Infrared Milli Terahz Waves, 38, pp. 1477–1486, 2017.
S. Kitagawa et al. "Wide frequency-tunable resonant tunnelling diode terahertz oscillators using varactor diodes," Electron. Lett., vol. 52, no. 6, pp. 479-481, 2016.
S. Kitagawa et al., "650-GHz Resonant-Tunneling-Diode VCO With Wide Tuning Range Using Varactor Diode," IEEE Electron Device Lett., vol. 35, no. 12, pp. 1215-1217, 2014.
J. Su, et al., “Wide frequency-tunable 1 THz resonant tunneling diode oscillator,” Int. Conf. Infrared, Millimeter and Terahertz Waves (IRMMW-THz), Chengdu, China, WE-AM-6-1, 2021.

## Slide 7: RTD
補足情報
コメント：RTDは高周波で特に有利、VCOレンジも広い。高い周波数範囲でRFフロントエンド部だけRTDデバイスで置き換えられるか？
課題：電力効率について、現状のRTDから完全にRF出力を取り出せた場合、~10%の効率が期待されるため、回路の最適化が必要。機能性を持たせるためにSi回路との集積化が課題。
変調など：直接ASK変調が可能で変調カットオフは高い（~30GHz）、複雑な変調（QAMなど）は現状できない。
パッケージ：Siレンズパッケージがよく用いられる。フォトニック結晶導波路や導波管接続もできるが、直接放射がパッチアンテナなどのオンチップアンテナも可能。
チップコスト：InP系のチップコストについては調査不足。。SiとInPでは10倍くらい？価格差がありそう。

## Slide 8: RTDの開発状況
Chart: Frequency (GHz)
| 450 | 1090 | 260 | 1980 | 1920 | 1000 | 1040 | 1420 | 1790 | 548 | 620 | 770 | 810 | 1520 | 675 | 1111 | 1220 | 500 | 1310 | 350 | 692 | 330 | 84 | 62.5 | 1550 | 1040 | 613 | 640 | 655 | 985
Output power (dBm) | #N/A | -20.46 | 0 | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | -27.21 | -13.28 | -40 | #N/A | #N/A | #N/A | #N/A | -20.32 | -11.55 | 3.01 | 5 | #N/A | #N/A | #N/A | #N/A | #N/A | -30
Output power (dBm) | 10.72 | #N/A | #N/A | -43.98 | -33.98 | -1.37 | -14.32 | -30 | -40 | -3.77 | -2.15 | -5.69 | -7.45 | #N/A | #N/A | #N/A | -21.55 | -6.58 | -20 | -15.09 | #N/A | #N/A | #N/A | #N/A | -33.98 | -21.55 | -19.21 | 0 | -21.74 | #N/A
Developed in Japan ( )
Other countries ( )
動作周波数が高く、~1THzまでは~mWの出力が可能
開発は日本が主導、他、イギリス、オーストリア、韓国など。近年、米国から報告はない。
Chart: Frequency (GHz)
| 450 | 1090 | 260 | 1980 | 1920 | 1000 | 1040 | 1420 | 1790 | 548 | 620 | 770 | 810 | 1520 | 675 | 1111 | 1220 | 500 | 1310 | 350 | 692 | 330 | 84 | 62.5 | 1550 | 1040 | 613 | 640 | 655 | 985
Output power (dBm) | #N/A | -20.46 | 0 | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | -27.21 | -13.28 | -40 | #N/A | #N/A | #N/A | #N/A | -20.32 | -11.55 | 3.01 | 5 | #N/A | #N/A | #N/A | #N/A | #N/A | -30
Output power (dBm) | 10.72 | #N/A | #N/A | -43.98 | -33.98 | -1.37 | -14.32 | -30 | -40 | -3.77 | -2.15 | -5.69 | -7.45 | #N/A | #N/A | #N/A | -21.55 | -6.58 | -20 | -15.09 | #N/A | #N/A | #N/A | #N/A | -33.98 | -21.55 | -19.21 | 0 | -21.74 | #N/A
36el.
89el.
2el.
Single
※帯は傾向を示す

## Slide 9: RTDの年次発展傾向
Chart: Year
| 2022 | 2022 | 2020 | 2017 | 2016 | 2019 | 2019 | 2014 | 2019 | 2011 | 2013 | 2013 | 2013 | 2015 | 2016 | 2011 | 2021 | 2022 | 2012 | 2021 | 2021 | 2021 | 2018 | 2014 | 2014 | 2010 | 2018 | 2016 | 2014 | 2021
Output power (dBm) | 10.72 | -20.46 | 0 | -43.98 | -33.98 | -1.37 | -14.32 | -30 | -40 | -3.77 | -2.15 | -5.69 | -7.45 | -27.21 | -13.28 | -40 | -21.55 | -6.58 | -20 | -15.09 | -20.32 | -11.55 | 3.01 | 5 | -33.98 | -21.55 | -19.21 | 0 | -21.74 | -30
Chart: Year
| 2022 | 2022 | 2020 | 2017 | 2016 | 2019 | 2019 | 2014 | 2019 | 2011 | 2013 | 2013 | 2013 | 2015 | 2016 | 2011 | 2021 | 2022 | 2012 | 2021 | 2021 | 2021 | 2018 | 2014 | 2014 | 2010 | 2018 | 2016 | 2014 | 2021
Frequency (GHz) | 450 | 1090 | 260 | 1980 | 1920 | 1000 | 1040 | 1420 | 1790 | 548 | 620 | 770 | 810 | 1520 | 675 | 1111 | 1220 | 500 | 1310 | 350 | 692 | 330 | 84 | 62.5 | 1550 | 1040 | 613 | 640 | 655 | 985
動作周波数は~2THzまで。周波数としてはすでに十分
出力は年々増加傾向、2030年代では~20dBmが期待（動作周波数が異なるが、おおよそとして）

## Slide 10: RTDの電力効率・面積効率
500GHz以下では1%以上の効率が期待される
出力密度（チップの単位面積あたりの出力）が260GHzで~10mW/mm2と大きい
Chart: Frequency (GHz)
| 450 | 1090 | 260 | 1980 | 1920 | 1000 | 1040 | 1420 | 1790 | 548 | 620 | 770 | 810 | 1520 | 675 | 1111 | 1220 | 500 | 1310 | 350 | 692 | 330 | 84 | 62.5 | 1550 | 1040 | 613 | 640 | 655 | 985
DC-to-RF efficiency (%) | 1 | 0 | 0.7 | 0 | 0 | 0.007 | 0.11 | 0 | 0 | 0.01 | 0 | 0 | 0 | 0.0164 | 0.33 | 0 | 0 | 0 | 0 | 0 | 0.274 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Chart: Frequency (GHz)
| 450 | 1090 | 260 | 1980 | 1920 | 1000 | 1040 | 1420 | 1790 | 548 | 620 | 770 | 810 | 1520 | 675 | 1111 | 1220 | 500 | 1310 | 350 | 692 | 330 | 84 | 62.5 | 1550 | 1040 | 613 | 640 | 655 | 985
Power density (mW/mm2) | 1.1527 | 0 | 8.3333 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.0079212 | 0.42718 | 0 | 0 | 0 | 0 | 0 | 0.081488 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
※帯は傾向を示す
※帯は傾向を示す